| Transmitted Light |  |  |
| --- | --- | --- |
| Transparent Specimens Phase Objects Bacteria, Spermatozoa, Cells in Glass Containers, Protozoa, Mites, Fibers, etc. | Phase Contrast Differential Interference Contrast (DIC) Hoffman Modulation Contrast Oblique Illumination |  |
| Light Scattering Objects Diatoms, Fibers, Hairs, Fresh Water Microorganisms, Radiolarians, etc. | Rheinberg Illumination Darkfield Illumination Phase Contrast and DIC |  |
| Light Refracting Specimens Colloidal Suspensions powders and minerals Liquids | Phase Contrast Dispersion Staining DIC |  |
| Amplitude Specimens Stained Tissue Naturally Colored Specimens Hair and Fibers Insects and Marine Algae | Brightfield Illumination |  |
| Fluorescent Specimens Cells in Tissue Culture Fluorochrome-Stained Sections Smears and Spreads | Fluorescence Illumination |  |
| Birefringent Specimens Mineral Thin Sections Liquid Crystals Melted and Recrystallized Chemicals Hairs and Fibers Bones and Feathers | Polarized Illumination |  |
| Reflected Light |  |  |
| Specular (Reflecting) Surface Thin Films, Mirrors Polished Metallurgical Samples Integrated Circuits | Brightfield Illumination Phase Contrast, DIC Darkfield Illumination |  |
| Diffuse (Non-Reflecting) Surface Thin and Thick Films Rocks and Minerals Hairs, Fibers, and Bone Insects | Brightfield Illumination Phase Contrast, DIC Darkfield Illumination |  |
| Amplitude Surface Features Dyed Fibers Diffuse Metallic Specimens Composite Materials Polymers | Brightfield Illumination Darkfield Illumination |  |
| Birefringent Specimens Mineral Thin Sections Hairs and Fibers Bones and Feathers Single Crystals Oriented Films | Polarized Illumination |  |
| Fluorescent Specimens Mounted Cells Fluorochrome-Stained Sections Smears and Spreads | Fluorescence Illumination |  |